# September 14-16, 2023, Institute of Chemical Technology, Mumbai

Exploring an Eco-Friendly Green Route to Synthesize Mono and Diesters using Zirconium Amino Phosphonic Acid Catalyst

Brijesh Shah*

Division of Chemistry, School of Science, Navrachana University Vasna Bhayli Road,

Vadodara 391410, Gujarat, India, brijeshshah27@gmail.com brijeshkumars@nuv.ac.in

## Introduction:

Esterification is a pivotal process in industry, enabling the synthesis of plasticizers, perfumes, cosmetic fragrances, food flavors, paint diluents, and pharmaceutical, dye, and fine chemical intermediates. Traditional esterification catalysts like sulfuric acid, methanesulfonic acid, or p-toluenesulfonic acid have raised environmental and operational concerns due to their potential hazards, difficulties in handling, acidic wastewater generation, and complex catalyst recovery [1]. To address these issues, solid acid catalysts have emerged as a safer and more environmentally friendly alternative, eliminating the corrosive nature of liquid acids. Among these alternatives, zirconium amino phosphonic acid has shown promise as an efficient and sustainable catalyst for esterification reactions. As a part of the global effort to promote greener and more sustainable synthesis pathways, this study investigates the feasibility of utilizing zirconium amino phosphonic acid catalysts in the production of mono and diesters, contributing to a more environmentally conscious approach in the synthesis of valuable chemical compounds. Numerous solid acid catalysts have been investigated for esterification reactions, as documented in literature sources [1]. These catalysts offer notable benefits, including straightforward work-up procedures and the ability to be regenerated and reused. Nevertheless, certain drawbacks have been observed, such as the leaching of active components from the catalyst, prolonged reaction times, the requirement for substantial catalyst quantities, and unsatisfactory yields of the ester product. Consequently, there is a pressing demand for an optimal solid acid catalyst that can overcome these limitations and enhance the efficiency of esterification processes. Tetravalent Metal Acid (TMA) salts are a class of inorganic cation exchangers with a general formula M(IV)(HXO4)2.nH2O, where M(IV) represents elements like Zr, Ti, Sn, Ce, Th, and X stands for elements such as P, W, Mo, As, Sb, etc. The structural hydroxyl groups in TMA salts contribute to cation exchange, making them promising candidates for solid acid catalyst applications, characterized by Bronsted acid sites [19,20]. The surface modification of TMA salts through the attachment of organic units is particularly intriguing. Treatment of tetravalent metal with phosphonic acids results in the formation of metal M(IV) phosphonates, wherein the PO(OH)3 group in the tetrahedral moiety is substituted with R (alkyl or aryl moiety) containing various functional groups like amino, alcoholic, carboxylic, sulfonic, etc. These hybrid materials, known as inorganic-organic hybrids, offer unique properties and potential applications. Zr - amino tris(methylenephosphonic acid) (Zr-ATMP) has been studied as an ion exchanger in water treatment, demonstrating effectiveness in removing various metal ions from water. However, there are no existing reports on the utilization of Zr-ATMP as a solid acid catalyst for organic transformations. Hence, this current study focuses on the synthesis of a claw type metal phosphonate, namely zirconium-aminophosphonic acid (Zr-ATMP), following a previously documented method [2]. Given that ATMP contains six structural hydroxyl groups, more than traditional phosphoric acid, it is expected that the resulting metal phosphonate will offer a higher density of catalytically active sites due to these pendant hydroxyl groups. The viability of these materials as solid acid catalysts has been investigated through the examination of esterification as a model reaction. In this context, the synthesis of both monoesters, including ethyl acetate (EA), propyl acetate (PA), butyl acetate (BA), and benzyl acetate (BzA), as well as diesters, such as diethyl malonate (DEM), diethyl succinate (DES), dioctyl phthalate (DOP), and dibutyl phthalate (DBP), has been carried out. The catalytic performance of the synthesized materials has been systematically compared and correlated with their respective acid properties.

## Material and Methods:

2.1 Synthesis of Zr-ATMP

The material was synthesized as per the reported conditions, Zr-ATMP was obtained as white hard granules. The synthesized material was characterized by various techniques in order to confirmed the composition of the material.

2.2 Catalytic Activity

## 2.2.1 Synthesis of mono esters

## In a typical reaction, a 100 mL round bottomed flask equipped with a Dean and Stark apparatus, attached to a reflux condenser was used and charged with acetic acid (0.050 - 0.075 M), alcohol (0.050 - 0.075 M), catalyst (0.05 - 0.20 g) and a suitable solvent (10 mL).  The reactions were carried out varying several parameters such as reaction time, catalyst amount, mole ratio of reactants and these parameters optimized. The temperature parameter has not been varied as the reaction temperature is sensitive to boiling points of reactants [ethanol (78°C), 1-propanol (97°C), 1-butanol (118°C) and benzyl alcohol (205°C)] as well as solvents used as azeotrope. Cyclohexane (b.p. 80°C) was used as a solvent for the synthesis of EA and toluene (b.p. 110°C) for PA, BA and BzA. After completion of reaction, catalyst was separated by decantation and reaction mixture was distilled to obtain the product.

## 2.2.2 Synthesis of diesters

## The diesters have been synthesized in two steps. The mono ester was prepared in first step by taking equimolar proportion (0.025 M) of acid and alcohol (malonic acid and ethanol for DEM, succinic acid and ethanol for DES, phthalic anhydride and 1-butanol for DBP, phthalic anhydride and 2-ethyl-1-hexanol for DOP) were taken in a round bottomed flask and the reaction mixture stirred at ~80°C for DEM and DES, ~115°C for DBP and ~140°C for DOP for about 10-15 min in absence of any catalyst and solvent. The dicarboxylic acid and anhydride gets completely converted to the monoester, so that the acid concentration at this stage is taken as the initial concentration. The obtained product (monoester) was then subjected to esterification reaction by addition of a second mole (0.025 M) of respective alcohol, catalyst (0.10 - 0.25 g) and 10 mL solvent (toluene (b.p. 115°C) for DEM, DES and DBP, and xylene (b.p. 140°C) for DOP). The reactions were carried out optimizing several parameters such as reaction time, catalyst amount and mole ratio of reactants. The temperature parameter has not been varied as discussed in synthesis of monoesters. In all cases the round bottomed flask was fitted with Dean and Stark apparatus, with a condenser to remove water formed during the reaction. After completion of reaction, catalyst was separated by decantation and reaction mixture was distilled to obtain the product.

## Significant Results and Discussion

3.1 Synthesis of mono esters:

The equilibrium constants of esterification reactions are relatively low. As with any equilibrium reaction, the direction of the reaction can be favorably shifted toward the product side by manipulating the concentration of one of the reactants (according to Le Chatelier's Principle) or by removing the water produced. In this study, a solvent mixture of cyclohexane/toluene was utilized to remove the water formed during the reaction in the form of a binary azeotrope using the Dean and Stark apparatus, thereby preventing the reverse reaction. The optimization of reaction conditions for the synthesis of ethyl acetate (EA) was carried out using Zirconium 1-amino-1,1-diphosphonate (ZrATMP) as a solid acid catalyst. Parameters such as reaction time, catalyst amount, and initial mole ratio of reactants were varied to determine their influence on the reaction yield.

## Table 1: Optimization of reaction conditions for synthesis of EA using ZrATMP

| Substrates (mole ratio) | Product formed | Catalyst amount (g) | Reaction temperature(oC)* | Reaction time (h) | % yield |
| --- | --- | --- | --- | --- | --- |
| Reaction time variation |  |  |  |  |  |
| E:AA (1:1) | EA | 0.05 | 80 | 1 | 34.82 |
| E:AA (1:1) | EA | 0.05 | 80 | 2 | 42.01 |
| E:AA (1:1) | EA | 0.05 | 80 | 3 | 43.90 |
| E:AA (1:1) | EA | 0.05 | 80 | 4 | 40.13 |
| E:AA (1:1) | EA | 0.05 | 80 | 5 | 42.34 |
| E:AA (1:1) | EA | 0.05 | 80 | 6 | 43.72 |
| E:AA (1:1) | EA | 0.05 | 80 | 7 | 52.62 |
| E:AA (1:1) | EA | 0.05 | 80 | 8 | 63.98 |
| E:AA (1:1) | EA | 0.05 | 80 | 9 | 64.06 |
| E:AA (1:1) | EA | 0.05 | 80 | 10 | 64.09 |
| Reaction temperature variation |  |  |  |  |  |
| E:AA (1:1) | EA | 0.05 | 115 | 8 | 46.55 |
| Catalyst amount variation |  |  |  |  |  |
| E:AA (1:1) | EA | 0.10 | 80 | 8 | 62.00 |
| E:AA (1:1) | EA | 0.15 | 80 | 8 | 63.30 |
| E:AA (1:1) | EA | 0.20 | 80 | 8 | 65.80 |
| Mole ratio variation |  |  |  |  |  |
| E:AA (1.5:1) | EA | 0.15 | 80 | 8 | 22.05 |
| E:AA (1:1.5) | EA | 0.15 | 80 | 8 | 76.92 |

(* Cyclohexane was used as solvent at 80oC and toluene was used at 115oC; E: Ethanol; AA: Acetic acid)

The results showed (Table 1) that the percentage yield of the product increased with longer reaction times (1-10 hours), but the gain in product after 8 hours was marginal. Increasing the amount of catalyst (0.05g - 0.20g) resulted in a proportional increase in the percentage yield, likely due to the greater availability of active sites. The impact of the reactant mole ratio on the reaction was also investigated by varying the mole ratio from 1:1.5 to 1.5:1 (acid:alcohol). The data from the study revealed that the % yield of the ester increased with a higher mole ratio of acid, while it decreased with an increasing mole ratio of alcohol. This phenomenon was attributed to the preferential adsorption of alcohol on the catalyst, leading to the blocking of active sites. For economic reasons, the less expensive reactant of the two is often used in excess. In this case, acids were used in excess, resulting in higher yields of the monoesters, and the excess acid also acted as a catalyst, further promoting the reaction. After optimizing the conditions (mole ratio of reactants = 1:1.5 (alcohol:acid); catalyst amount = 0.15g; reaction time = 8 hours), the synthesis of various esters, PA, BA, and BzA, was carried out using ZrATMP. It was found that the synthesis of monoesters EA, PA, and BA without a catalyst led to poor yields, emphasizing the necessity of a catalyst for these reactions. In the case of BzA, high yields were observed even in the absence of a catalyst when there was an excess of acetic acid, which was attributed to auto-catalysis. The % yield of esters formed (Table 2) followed the order BzA > BA > EA > PA, and the turn over number (TON) of the catalyst also followed the same order, reflecting the effectiveness of the catalyst. The higher yields of BzA could be attributed to the enhanced nucleophilicity due to the presence of an aromatic ring in benzyl alcohol. In a different report, high yields of BzA were achieved with a small amount of catalyst, but the reaction time was relatively long. It was explained that when the boiling point of the alcohol is lower than the reaction temperature, a significant portion of the alcohol will be in the vapor phase and not available for the reaction in the liquid phase. Consequently, heavier alcohols tend to react more readily than lighter ones.

Table 2 Synthesis of mono esters at optimized condition using ZrATMP

| Catalytic run | Yields of mono ester (%) / (TON) |  |  |  |
| --- | --- | --- | --- | --- |
|  | EA | PA | BA | BzA |
| 1 | 79.92(34.97) | 58.95(28.45) | 84.92(45.87) | 87.35(57.65) |
| 2 | 79.11(34.14) | 58.44(27.76) | 82.11(44.88) | 86.00(56.69) |
| 3 | 79.98(33.18) | 57.90(26.95) | 81.68(44.65) | 83.69(55.17) |

(Mole ratio Acid:Alcohol=1.5:1, Reaction temperature: 800C for EA, 115oC for PA, BA and BzA; Reaction time: 8 h;

Amount of catalyst: 0.15g; Solvent: cyclohexane for EA and toluene for PA, BA and BzA)

3.2 Synthesis of diesters:

Diesters DEM, DES, DOP, and DBP were synthesized in two steps. The first step is so rapid, that it can be carried out in the absence of catalyst attributed to the fact that, the electron withdrawing effect of one carboxyl group enhances the ionization of the other causing the -COOH groups to be protonated in this region of pH [3]. However, esterification of the second carboxylic group (second step) is very slow and needs to be facilitated by acid catalyst wherein the resulting water must also be removed from the reaction mixture [3]. Reaction conditions were optimized (Table 3) using ZrATMP as solid acid catalysts for DEM synthesis by varying various parameters as mention early.

## Table 3 Optimization of reaction conditions for synthesis of DEM using ZrATMP

| Substrates (mole ratio) | Product | Catalyst amount (g) | Reaction temperature (oC)* | Reaction time (h) | % yield |
| --- | --- | --- | --- | --- | --- |
| Reaction time variation |  |  |  |  |  |
| E:MA (2:1) | DEM | 0.10 | 115 | 1 | 74.35 |
| E:MA (2:1) | DEM | 0.10 | 115 | 2 | 75.44 |
| E:MA (2:1) | DEM | 0.10 | 115 | 3 | 76.64 |
| E:MA (2:1) | DEM | 0.10 | 115 | 4 | 78.25 |
| E:MA (2:1) | DEM | 0.10 | 115 | 5 | 80.49 |
| E:MA (2:1) | DEM | 0.10 | 115 | 6 | 82.36 |
| E:MA (2:1) | DEM | 0.10 | 115 | 7 | 83.79 |
| E:MA (2:1) | DEM | 0.10 | 115 | 8 | 83.87 |
| E:MA (2:1) | DEM | 0.10 | 115 | 9 | 83.96 |
| E:MA (2:1) | DEM | 0.10 | 115 | 10 | 84.23 |
| Catalyst amount variation |  |  |  |  |  |
| E:MA (2:1) | DEM | 0.15 | 115 | 8 | 88.46 |
| E:MA (2:1) | DEM | 0.20 | 115 | 8 | 89.77 |
| E:MA (2:1) | DEM | 0.25 | 115 | 8 | 90.97 |
| Mole ratio variation |  |  |  |  |  |
| E:MA (2.2:1) | DEM | 0.15 | 115 | 8 | 88.24 |
| E:MA (2.4:1) | DEM | 0.15 | 115 | 8 | 87.56 |

(*Solvent used: Toluene; E: Ethanol; MA: Malonic acid)

At optimized conditions (mole ratio of reactant = 1:2 (acid/anhydride: alcohol), catalyst amount = 0.15 g and reaction time = 8 h) synthesis of other diesters was performed using ZrATMP (Table 4). In the present work, % yield of diester formed is observed to be DEM > DES > DOP > DBP. The yields of DOP are higher than DBP which could be attributed to higher boiling point of 2-ethyl-1-hexanol compared to 1-butanol. High yields in the case of DEM and DES, compared to DOP and DBP is probably due to less steric hindrance felt by incoming ethanol from monoester formed in the first step.

Table 4 Synthesis of diesters at optimized condition using ZrATMP

| Catalytic run | Yields of diester (%) / (TON) |  |  |  |
| --- | --- | --- | --- | --- |
|  | DEM | DES | DOP | DBP |
| 1 | 92.10 (30.02) | 88.84 (31.03) | 84.00 (57.12) | 68.02 (33.55) |
| 2 | 90.13 (29.38) | 87.08 (30.41) | 83.12 (56.52) | 67.61 (33.35) |
| 3 | 89.41 (29.14) | 85.12 (29.37) | 82.78 (56.29) | 65.69 (32.40) |

(Mole ratio Acid:Alcohol=1:2, Reaction temperature: 1150C for DEM, DES and DBP, 140oC for DOP; Reaction time: 8 h;

Amount of catalyst: 0.15g; Solvent: xylene for DOP and toluene for DEM, DES and DBP)

## Conclusions:

The work presented herein, reveals the promising use of ZrATMP as solid acid catalyst in the synthesis of mono and diesters, the advantages being operational simplicity, mild reaction conditions and environment friendly nature of the catalyst. However, due to excellent catalytic performance, 87.64% yield of BzA and 92.10% yield of DEM has potential for commercialization.

References

[1] F. T. Sejidov, Y. Mansoori, N. Goodarzi, J. Mol. Catal. A: Chem., 240,2005, 186-190.

- B. Shah and U. Chudasama, Desalination and Water Treatment 38,2012, 227–235.

- M. Arabi, J. Mol. Catal. A: Chem., 200 (2003) 105-110.