# September 14-16, 2023, Institute of Chemical Technology, Mumbai

Alkylation of phenol and thiophenol with various alkenes using ion exchange resin catalyst

Prerana Masurkar1, Pravin Jadhav2, Sunil Mokashi2, Shirish Naik2, Manoj Bhandari2, Dinesh Mandhan2, Bhalchandra M. Bhanage*1

1Department of Chemistry, Institute of Chemical Technology, N. Parekh Road, Matunga, Mumbai 400019

2Thermax Limited, MIDC, Bhosari, Pune 411026.

E-mail addresses: bm.bhanage@ictmumbai.edu.in, dinesh.mandhana@thermaxglobal.com

## 1. Introduction

Catalysts are required for important organic processes to be employed industrially or academically. In this aspect, ion exchange resin catalysts surpass typical inorganic catalysts, particularly in terms of product separation from the reaction media, recycling, and recycling. Ion-exchange resins are solid acid heterogeneous catalysts that play a vital role in many advantageous reactions such as alkylation, esterification, etherification of olefins with alcohols, dehydration of alcohols to olefins or ethers, olefin hydration, and ester hydrolysis. Alkylation is the transfer of an alkyl group from one molecule to another, and it is one of the most significant catalytic processes in the chemical industry since it is widely used in industries such as fuels, cleaning products, and pharmaceuticals. The primary issue with existing industrial processes is environmental contamination, which also causes facilities to deteriorate. For this reason, it is anticipated that a new kind of solid acid catalyst will be developed to replace conventional catalysts that is well-behaved and environmentally friendly [1]. Strongly acidic ion-exchange sulfonic acid resins have been extensively exploited as recyclable acid catalysts for organic syntheses in both laboratory and industry since they became commercially available. The "principles of green chemistry" are in fact compatible with catalytic recycling. Among the various solid acid catalysts investigated, ion exchange resins have attracted much attention because of their suitable acidity, regeneration, reuse and simplified product recovery and reduction of undesirable waste streams [2].

Herein, we have studied the alkylation of phenol and thiophenol with various alkenes to produce alkyl phenol and alkyl thiophenol by using TULSION T-6813 MP as a catalyst [3]. The present work reviews the progress on alkylation of phenol and thiophenol using TULSION T-6813 MP ion exchange resin. Influence of ion exchange resin on final yield is elaborated. The detailed mechanistic perspectives of alkylation with phenol and thiophenol in presence of strong acidic catalytic system is emphasized in the article. The understanding of catalytic behavior through reaction kinetic analysis is described. The selection of suitable catalyst with appropriate process parameters is very important in commercialization of any process. These insights are useful to develop synthesis strategies towards new and or improved catalysts, predict more realistic reaction conditions for selective product formation and design industrial catalytic reactor systems.

- Materials

The TULSION T-6813 MP was supplied by Thermax Limited (Mumbai, India). Ion exchange resin catalysts were thoroughly washed with double distilled water. Subsequently, resin catalysts were dried in a dryer at 80°C for minimum 12 h and in a vacuum dryer for another 4 h at the same temperature up to the point where <2% moisture were detected.

All chemicals and reagents were obtained from Sigma Aldrich and Spectrochem Pvt. Ltd. Characterisation of product was done by 1H-NMR spectra. Progress of reaction was monitored by gas chromatography (Perkinelmer, Clarus 580) (TG-5 MS GC column, 30 m length, 0.25 mm ID, film thickness 0.25 µm). Products were confirmed by GC-MS (Shimadzu GC-MS QP 2010).

2. Experimental procedure

2.1 Procedure for alkylation of phenol with alkene

The alkylation reaction was performed using a 50 mL three-neck reactor fixed with a glass stirrer, reflux condenser, and thermometer. A measured quantity of resin catalyst (12 % of alkene) was taken in the reactor and the reactor was placed in an oil bath. A measured quantity of alkene and phenol (1:2 mole) was added to the flask, the reaction mixture was heated to 90°C, and then maintained at the same temperature (90°C) for 4 hours. Maintained the stirring speed so as to keep slurry moving without spurting. After the reaction completion, the mixture was added into a sample collector, and the supernatant sample was forwarded for GC analysis. The structure of the product was determined by GC-MS and 1H-NMR.

  - Procedure for alkylation of thiophenol with alkene

The alkylation reaction was performed using a 50 mL three-neck reactor fixed with a glass stirrer, reflux condenser, and thermometer. A measured quantity of resin catalyst (12 % of alkene) was taken in the reactor and the reactor was placed in an oil bath. The measured quantity of alkene and thiophenol (1:2 mole) was added to the flask, the reaction mixture was heated to 90°C, and then maintained at the same temperature (90°C) for 4 hours. Maintained the stirring speed so as to keep slurry moving without spurting. After the reaction completion, the mixture was added into a sample collector, and the supernatant sample was forwarded for GC analysis.

3. Results and Discussion

3.1 Characterization of catalyst

The surface area and porosity of the products were determined by nitrogen adsorption/desorption analysis and mercury porosimetry. The instrument utilized for nitrogen sorption analysis was a Micromeritics Gemini VII Surface Area and Porosity analyzer. The specific surface area of the dry resins was determined using the nitrogen sorption BET technique and the pore size distribution was determined by the BJH model. Mercury porosimetry was carried out using a Micromeritics AutoPore IV 9500 instrument. The Agilent Cary 60 UV-Vis spectrophotometer was used for color leaching analysis and results of resin sample shows in Table 1.

Table 1: Surface area, porosity and pore diameter of three resin samples.

| Ion exchange resin | Surface area, m2/g | Porosity, % | APD, Å |
| --- | --- | --- | --- |
| TULSION T-6813 MP | 35.58 | 33.39 | 267 |

APD: average pore diameter

## 3.2 Analysis of reaction conditions

## We have selected alkylation of phenol with nonene as a model reaction and influence of various parameters such as temperature, solvent, reaction time, catalyst concentrations, catalyst loading was studied. We have used various solvents for this reaction but, reaction gives good yield in solvent free conditions. To determine catalyst concentration, Substrate ratio 2:1 (phenol: 1-nonene) gives good yield of product. In a pursuit of determining the optimal concentration of the catalyst, the catalyst concentrations varied ranging from 5 to 12 % w/w. The best results were obtained from 12 % w/w concentration of the catalyst. Parameters like temperature and reaction time were also studied. The optimal temperature for the reaction is 90°C and the time required for maximum conversion was 4h. Therefore, based on the experimental results, TULSION T-6813 MP was found to be the best catalyst for phenol and thiophenol alkylation reaction.

## Table 1: Optimization conditions for alkylation reactions using TULSION T-6813 MP as a catalyst

| ## Entry | ## Solvent | ## Temperature, °C | ## Time, Hrs | ## Yield |
| --- | --- | --- | --- | --- |
| ## 1 | ## Acetonitrile | ## 90 | ## 4 | ## 10 |
| ## 2 | ## 1,2-Dichloroethane | ## 90 | ## 4 | ## - |
| ## 3 | ## Anisole | ## 90 | ## 4 | ## 15 |
| ## 4 | ## Toluene | ## 90 | ## 4 | ## 20 |
| ## 5 | ## Without solvent | ## 80 | ## 4 | ## 75 |
| ## 6 | ## Without solvent | ## 100 | ## 4 | ## 88 |
| ## 7 | ## Without solvent | ## 120 | ## 4 | ## 85 |
| ## 8 | ## Without solvent | ## 90 | ## 4 | ## 95 |
| ## 9 | ## Without solvent | ## 90 | ## 2 | ## 80 |
| ## 10 | ## Without solvent | ## 90 | ## 3 | ## 85 |

After optimization various derivatives of phenol and alkenes were investigated for alkylation reaction and were found to furnish good to excellent yields of the desired products. After successful alkylation of phenol, we have used similar reaction conditions for S-alkylation of thiophenol. Different thiophenol with electron donating and withdrawing group were reacted with various alkenes. Products were obtained in excellent yield (75-95 %).

Conclusions:

Alkylation of phenol and thiophenol with various alkenes using catalyst TULSION T-6813 MP were studied. Catalyst is inexpensive, efficient and recyclable. Higher yields of desired products within a short reaction time under solvent free conditions was obtained. It was found experimentally that the TULSION T-6813 MP give the best performance for the alkylation of phenol and thiophenol.

References

- D.A. Pisanenko, Y.I. Smirnov-Zamkov, Alkylation of phenol with olefins in the presence of lignosulfonic acids, Russ. J. Appl. Chem. 72 (1999) 1655–1657.

- M.A. Freire, et al., Acid-catalyzed liquid-phase alkylation of phenol with branched and linear olefin isomers, Catal. Today (2016).

- Ziyauddin S. Qureshi, Krishna M. Deshmukh, Kishor P. Dhake and Bhalchandra M. Bhanage*, RSC Adv., 2011, 1, 1106–1112