# September 14-16, 2023, Institute of Chemical Technology, Mumbai

Synthesis of biofuel additives from bio platform molecules over 12-tungstophosphoric acid anchored to zeolite HY

Margi Joshi1, Anjali Patel2

1Polyoxometalates and Catalysis Laboratory, Department of Chemistry, Faculty of Science, The Maharaja Sayajirao University of Baroda

2Polyoxometalates and Catalysis Laboratory, Department of Chemistry, Faculty of Science, The Maharaja Sayajirao University of Baroda

E-mail address: margisjoshi761@gmail.com, anjali.patel-chem@msubaroda.ac.in

## Introduction:

The global trend toward an extensive cultivation of biofuel production is one of historical significance. This is a result of the rising consumption of non-renewable petroleum resources, which calls for advances in contemporary technology to employ renewable resources [1]. The transformation of biomass derivatives into valuable molecules has become crucial from both a financial and ecological standpoint. An approach towards this brings focus on 12 bio platform molecules. Among, alkyl esters of levulinic acid and succinic acid are known to be important biofuel additives.

Scheme 1. C4 and C5 bio platform molecules and their applications

## Material and Methods:

All materials used were of A.R. (analytical) grade. Levulinic acid, Succinic acid, n-butanol, 12-tungstophosphoric acid, Dichloromethane, Methanol were purchased from Merck. Zeolite NaY was acquired commercially from Reliance Industries Limited, Vadodara, Gujarat. The catalyst was synthesized in two steps, i) Conversion of zeolite NaY to HY by ion exchange method [2] ii) PW12 was anchored to ZHY by incipient wet impregnation method. The synthesized materials were characterized by acidity measurements, FTIR, BET, EDX, TGA, 31P NMR, XRD and HRTEM. Further, PW12/ZHY was used for the synthesis of fuel additives which was carried out in a simple batch reactor. Consequently, the effect of various reaction parameters such as mole ratio, catalyst amount, time, and temperature were studied to optimize the conditions for maximum conversion.

# September 14-16, 2023, Institute of Chemical Technology, Mumbai

## Significant Results and Discussion

BET analysis shows the successful anchoring of PW12 into the pores of ZHY. The FTIR spectra indicates the intact structure of Keggin ion in the catalyst while, TGA shows the stability of the catalyst. The XRD and HRTEM reveals the uniform dispersion of PW12 inside the pores of ZHY. For instance, HRTEM images of ZHY and PW12/ZHY are shown in Figure 1.

Figure 1. HRTEM images of support and catalyst

The catalytic activity of PW12/ZHY towards esterification of levulinic acid as well as succinic acid with n-butanol was evaluated [2,3]. The superiority of the present work lies in getting very high conversion and selectivity for both the biofuel additives n-butyl levulinate and dibutyl succinate under mild conditions.

Table 1. Conversion and Selectivity

| Esterification of bio platform molecules |  |  |  |
| --- | --- | --- | --- |
| Bio platform molecules | % Conversion | %Selectivity |  |
|  |  | n- butyl levulinate | Dibutyl succinate |
| Levulinic acid | 88 | 99 | NA |
| Succinic acid | 92 | NA | 60 |

## Conclusions:

A novel sustainable heterogeneous catalyst comprising 12-tungstophosphoric acid and zeolite HY demonstrating excellent catalytical performance in a solvent-free esterification reaction. Moreover, the removal of the catalyst consists of a single filtration and the catalyst can be reused after a simple work-up.

References

[1] KC Badgujar, BM Bhanage, Fuel Process Technol, 2015, 138,139–146.

[2] A. Patel, M. Joshi, S. Sharma, Biomass Conv and Bioref., 2022.

[3] A. Patel, M. Joshi, Energy fuels, 2023, 37, 13, 9247-9256.